**Amendments to Specification 3.53, Asphalt Concrete Pavement - Superpave**

1. Subsection 3.53.1.2.14, **QA Acceptance Lot** is replaced in its entirety with the following:

A Lot in which all acceptance testing is conducted by the Consultant using quality assurance test procedures as outlined in these specifications. The number and selection of QA Acceptance Lots shall be determined as follows:

1. First two Lots of production for each Mix Type used, except for Mix Type S1 in which case the first Lot shall be used, and;
2. One additional random Lot for the bottom lift, if two or more lifts are specified, and;
3. Minimum of one additional random Lot per 20,000 tonnes, or portion thereof, of total ACP contract tender tonnage and;
4. Three additional random Lots of top lift production, for each Mix type, if two or more lifts are specified and;
5. Any additional Lot(s) chosen by the Consultant.
6. Subsection 3.53.2.4, **Reclaimed Asphalt Pavement**, replace the last paragraph in its entirety with the following:

For RAP/virgin aggregate blends greater than 10/90, the Contractor shall adjust the virgin asphalt grade and/or undertake rheology testing of the RAP and virgin asphalt cements according to the requirements listed in Table 3.53.2.4 Asphalt Grade Adjustment and Rheology Testing for RAP Usage. Rheology testing of the blended RAP and virgin asphalt cements shall meet the requirements of the specified grade.

1. Replace the following sentence in Sub Section 3.53.5.4 **Placing the Mix,**

*“If required by the Consultant the contact edge of any mat placed by the Contractor shall be coated with a thin film of liquid asphalt before placing the adjacent mat.”*

In its entirety, with the following:

The contact edge of any mat placed by the Contractor shall be coated with a thin film of liquid asphalt before placing the adjacent mat.